----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.  If you do not wish to receive news releases from us or you are not the proper contact for news releases please email us at newsrelease@masterbond.com.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.

----------------------------------

FOR IMMEDIATE RELEASE

High Temperature Resistant Epoxy Offers

Outstanding Chemical Resistance

HACKENSACK, NJ - Mar 10, 2003 -- Master Bond Inc. of Hackensack, New Jersey has developed a new two component epoxy system for service above 500°F.  Called EP125, this compound is designed to withstand exposure to boiling acids, alkalis, salts, fuels and most organic solvents.  It offers high bond strength to metallic and nonmetallic surfaces.  Typical lap shear strengths are in the order of 2,400-2,500 psi at ambient temperatures.  After heat aging for 1,000 hours at 500°F, slightly less than 50% of the original bond strength is retained.  Castings exhibit flexural strength as high as 15,000 psi and flexural moduli of more than 500,000 psi.

Master Bond EP125 has a convenient mix ratio of 2 to 1 by weight.  It requires an elevated temperature cure.  Cure cycles can be widely adjusted so as to best meet specific processing needs.  It has a storage stability of 6 months when stored at ambient temperatures in the original closed containers.  EP125 is available in 1/2 pint, pint, quart, gallon and 5 gallon pail kits.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #